Lifetime measurement check list:

Preparation:

- Clean the chamber if needed.

- Bake the chamber

  - Time needed to bake it

  - Temperature needed to bake it around 200°C because of the O-ring

- Check the pressure using RGA

  - Total pressure

  - Pressures for oxygen and water (they should be smaller than 10-9 Torr)

- Anode

  - Material (nickel, stainless steel, etc.)

  - Procedure to clean nickel anode:

    - Mechanically polish the nickel anode;

    - Electropolishing the nickel anode;

    - Annealing the nickel anode at 1000 °C for two days.

During the measurement:

- Distance between anode and cathode;

- External resistance;

- Duty cycle;

- Frequency;

- Pulse width;

- Voltage range;

- Voltage compensation step;

- Emission current;

- Lifetime;

After the measurement:

- Pressure using RGA

  - Total pressure;

  - Pressures for oxygen and water (should be smaller than 10-9 Torr)

SEM should be used to characterize the morphology of the cathode before and after the lifetime measurement.